# Memory-Efficient Geant4 Modelling Regimes for Nanocomposite Radiation Shielding: Effective Medium, Explicit Nanoparticle Geometry, and Hybrid Representative-Volume Validation

Hani H. Negm¹

¹ Department of Physics, [AFFILIATION REQUIRED — DO NOT SUBMIT WITH PLACEHOLDER]

Corresponding author: [email]

Manuscript version: v04 (v03-r4 → v04: Phase 4 internal audit applied — abstract RVE wording, H1 energy qualifier, §4.2 beam description, §5.1.3 EPDL97 citation, §5.2.2 stale note removed, §3.3 feasibility note, §8 limitations updated; figure style guide compliance applied)

Target journals (Q1, in priority order): 1. Radiation Physics and Chemistry (Elsevier, IF ≈ 2.9; primary scope match — shielding + MC methodology) 2. Nuclear Instruments and Methods in Physics Research A (NIM A, Elsevier; established Geant4 methods venue) 3. Computer Physics Communications (Elsevier; physics + software methodology) 4. Physics in Medicine and Biology (IOP; if diagnostic-energy nano-dose results are emphasised) 5. Annals of Nuclear Energy (Elsevier; if shielding-engineering framing is emphasised)

## Abstract

Nanoparticle-loaded radiation-shielding materials are routinely simulated in Geant4 as elemental homogeneous mixtures, despite the term nanocomposite implying a resolved microstructure. The validity boundary of this homogenisation has not been systematically mapped against the explicit-geometry alternatives that Geant4 actually supports, and the computational cost of moving beyond homogenisation is rarely quantified. This paper presents a controlled benchmark of three Geant4 modelling regimes applied to an HDPE/Bi₂O₃ nanocomposite at volume fraction ϕf=0.189 (68.6 wt% Bi₂O₃, ρeff=2.452 g cm​−3, derived from the linear mixture rule with pure-phase densities ρf=8.9 and ρm=0.95 g cm​−3): (A) effective-medium mass-fraction G4Material; (B) explicit nanoparticle placement via G4PVParameterised inside a 1 µm representative-volume-element (RVE) cube; and (C) voxelised G4MultiUnion inclusion clusters inside a 250 nm RVE (N=45 spheres). All three regimes use the same Geant4 11.4 build, the same physics list (G4EmLivermorePhysics), and a matched photon energy grid spanning 30 keV–1.33 MeV. The primary endpoint is the mass attenuation coefficient μ/ρ(E) compared against NIST XCOM.

Two regime-A (effective-medium) benchmarks are reported: (i) an XCOM validation run at 30 wt% Bi₂O₃ (ρ=2.45 g cm​−3, 106 histories per point) that yields mean and maximum absolute percent differences of 0.549% and 2.013% against XCOM, satisfying pre-registered acceptance thresholds; and (ii) a cross-regime companion run at the composition matching the RVE phases (68.6 wt% Bi₂O₃, ρ=2.452 g cm​−3, same energy grid), which serves as the regime-A baseline for the H1 test. Regimes B and C (explicit RVE, G4PVParameterised and G4MultiUnion respectively) use random-sequential-addition placement of Bi₂O₃ spheres (radius 25 nm, ϕf=0.189, 68.6 wt%) inside the RVE host; simulations are executed at 107 histories per energy point. Regime B (1 µm RVE, N=2,888 spheres) confirms effective-medium agreement within the 3% H1 gate at 30–150 keV (μB/μA,ϕ=0.975–0.984), correctly resolves the Bi K-edge jump (×2.3 at 100 keV), and agrees with NIST XCOM to within 1.6–4.0% at those energies. Regime C (250 nm RVE, N=45 spheres, G4MultiUnion, distributed beam sampling) confirms H1 at 30–150 keV (μC/μA,ϕ=0.982–1.016), with XCOM agreement of −2.3% to +1.2% at those energies. The G4Voxelizer memory scaling ((2N)3 cells) limits the feasible node count to N≲50 on an 8 GB workstation; this is characterised as a scalability finding. All three regimes are complete and the cross-regime comparison figure (Figure F-cross, A+B+C) has been generated.

Keywords: Geant4 · radiation shielding · nanocomposite · effective medium · G4MultiUnion · G4PVParameterised · representative volume element · mass attenuation coefficient · Monte Carlo benchmarking · reproducible workflow

## 1. Introduction

### 1.1 Background

Polymer-matrix radiation-shielding composites loaded with high-Z fillers (Bi₂O₃, WO₃, PbO, BaSO₄, Gd₂O₃) have become a sustained research focus over the past decade, driven by the need for lead-free, flexible, low-toxicity alternatives in medical X-ray protection, nuclear medicine, and aerospace shielding. A substantial fraction of the recent literature reports filler particle sizes in the nanometre range and labels the resulting materials as nanocomposites. When such materials are simulated in Monte Carlo (MC) transport codes — most commonly Geant4 [1–3] — the dominant practice is to define one G4Material from elemental mass fractions and a measured or estimated bulk density. The microstructure is not resolved.

This homogenisation is physically defensible for the macroscopic shielding regime in which the relevant photon mean free path (MFP) is orders of magnitude larger than both the filler particle radius and the inter-particle spacing. Under that condition the photon “sees” an effective medium and the Bragg–Gray mass-fraction additivity rule [4,5] yields linear attenuation coefficients consistent with NIST XCOM [6] to within the independent-atom approximation. The validity boundary of this rule has been extensively characterised for macroscopic mixtures [5,7], but the question that motivates this work is different: under what circumstances does the spatial arrangement of the high-Z phase, at the nanoscale, change a quantity that a shielding engineer or medical physicist actually cares about — transmission, broad-beam dose, or interface dose — by more than the experimental uncertainty?

### 1.2 Gap

Three gaps remain in the literature:

- Validity boundary of homogenisation. Although effective-medium MC results agree with experiment for many nanocomposite shielding measurements at gamma energies, there is no published systematic Geant4 benchmark that holds composition, density, source, scoring geometry, and physics list constant while varying only the geometric representation (homogeneous vs explicit-particle vs clustered) and reports the cross-method deviation as a function of photon energy and filler loading.

- Computational cost characterisation. The Geant4 Application Developer Guide documents G4PVParameterised and G4MultiUnion as standard constructs, but the practical scaling of runtime, memory, and geometry-construction time for radiation-shielding-relevant nanoparticle counts has not been mapped. Practitioners frequently assume that “Geant4 can do it” without quantifying when it cannot.

- Production-grade methodology. Existing nanoparticle-resolved Geant4 studies are concentrated in the nano-radiosensitisation/Geant4-DNA community [8,9,10], where the physical scale is sub-cellular and the particle counts are tractable. There is no published bridge between that microscopic methodology and the macroscopic shielding-engineering use case, where a representative volume element (RVE) approach is the only physically and computationally viable path.

### 1.3 Contribution and hypothesis

This paper contributes (i) a controlled three-regime benchmark for nanocomposite shielding in Geant4; (ii) a quantitative test of the effective-medium hypothesis against explicit nanoparticle geometry over a diagnostically relevant energy range; (iii) an open, reproducible benchmark harness released with ShieldLab G4 v1.1.

Hypothesis (H1). For photon energies where the photon mean free path greatly exceeds the nanoparticle radius (μr≪1, i.e., r≪1/μ), the transmitted fluence through the same material composition is independent of the choice of regime A, B, or C within the statistical uncertainty of 106–107-history Geant4 runs, provided composition, density, and scoring are matched.

Hypothesis (H2). For photon energies E≲100 keV with high-Z fillers (Bi₂O₃), the radial dose-enhancement profile around individual particles carries spatial structure that the effective-medium regime cannot reproduce.

Each hypothesis is operationalised as a numeric acceptance criterion in §4.5.

## 2. Theoretical Basis

### 2.1 When homogenisation is exact, when it is approximate, and when it fails

The mass-fraction additivity rule for the mass attenuation coefficient,

μρmix(E)=i​wiμρi(E),

is exact under the independent-atom approximation and the assumption that the photon interaction probability per unit mass is independent of the geometric distribution of atoms within the irradiated mass. This holds when:

- The photon de Broglie wavelength is small compared with inter-atomic spacing (true for all E>1 keV considered here).

- Coherent (Rayleigh) inter-particle interference is negligible (true above ~10 keV for amorphous nanocomposites).

- The penetration depth is large compared with any heterogeneity length scale (the macroscopic-homogenisation condition).

The third condition is the one that fails first for nanocomposites under low-energy, high-Z conditions.

### 2.2 Effective density

Geant4 requires density. All regimes in this paper use the same input density, computed from the volume-fraction rule of mixtures. Given filler volume fraction ϕf:

ρeff=ϕfρf+(1−ϕf)ρm

with ρm=0.95 g cm​−3 (HDPE) and ρf=8.9 g cm​−3 (Bi₂O₃). For the target composite density ρeff=2.45 g cm​−3, the filler volume fraction derived from the linear mixture rule is

ϕf=ρeff−ρmρf−ρm=2.45−0.958.9−0.95=0.189.

The corresponding filler mass fraction is wf=ϕfρf/ρeff=0.189×8.9/2.45=0.686 (68.6 wt% Bi₂O₃). This is the self-consistent high-loading formulation used for all three regimes in the cross-regime comparison. An additional regime-A validation run at 30 wt% (with the density left as a user-specified 2.45 g cm​−3 input) is also reported for XCOM verification of the emlivermore physics list independent of the density assignment.

### 2.3 The representative volume element

An RVE is the smallest cubic cell that statistically reproduces the bulk composite’s microstructure. For a random dispersion of monodisperse spheres of radius r at volume fraction ϕf, the mean inter-particle centre-to-centre distance is approximately

d≈r4π3ϕf1/3.

A practical RVE side length is LRVE≳5d. For r=25 nm and ϕf=0.189, d≈42 nm, so LRVE=1 µm satisfies the criterion and contains approximately 2,889 non-overlapping spheres — tractable for Geant4.

## 3. Geant4 Modelling Regimes

### 3.1 Regime A — Effective-Medium G4Material

Implemented in MaterialRegistry::AddMassFractionMaterialCommand in src/MaterialRegistry.cc. Compound formulae are expanded to elemental mass fractions using the analytical layer in python/shieldlab/core/materials.py, then a single G4Material is constructed:

auto* mat = new G4Material(name, rho_eff*g/cm3, nElements);
for (auto& e : elements) mat->AddElement(nist->FindOrBuildElement(e.symbol), e.fraction);

A 1-D slab geometry is built in src/DetectorConstruction.cc. Per-energy slab thickness is selected so that transmission is T≈0.65 at every energy point, maximising the sensitivity of the direct transmission estimator μ=−lnT/t.

Cost class: O(1) in particle count; identical to bulk-material runs.

### 3.2 Regime B — Explicit Nanoparticles via G4PVParameterised

Class NanoParticleParameterisation : public G4VPVParameterisation is implemented in include/NanoParticleParameterisation.hh and src/NanoParticleParameterisation.cc. Particle positions are sampled by random sequential addition (RSA) with a hard-sphere exclusion radius of 2r inside an RVE cube. The parameterisation is wrapped in a G4PVParameterised placement inside a matrix host logical volume:

new G4PVParameterised("NPParam", npLogic, rveLogic,
                      kUndefined, N, param);

The ComputeTransformation callback applies only a translation per copy; no rotation is needed for monodisperse spheres.

RVE geometry parameters (this study): side = 1 µm, r=25 nm, ϕf=0.189, max particles = 3,500, RSA seed = 22,222. RSA placed 2,888 / 2,888 target spheres (achieved ϕf=0.1890).

Scoring and output: The world and scoring infrastructure remain the same as regime A. The RVE host box acts as the “slab”; transmission is scored at the world exit face (±L/2 in x). GetTotalThickness() returns LRVE from the pseudo-layer record, so μ=−lnT/LRVE is computed identically to regime A.

Cost class: geometry navigation scales near-logarithmically with N thanks to voxelisation.

### 3.3 Regime C — G4MultiUnion Cluster

The same RSA particle list (seeded with 33,333 for an independent draw) is assembled into a single G4MultiUnion solid:

auto* fillerUnion = new G4MultiUnion("FillerUnion");
for (auto& pos : positions) {
    G4Transform3D tr(identity, pos);
    fillerUnion->AddNode(*sphereTemplate, tr);
}
fillerUnion->Voxelize();

A single G4PVPlacement is made into the RVE host box. This regime represents fixed-cluster placement and benchmarks how Geant4’s internal multi-union voxelisation scales relative to parameterised placement.

In practice, G4MultiUnion::Voxelize() is only feasible for N≲50 on 8 GB hardware; §5.3 documents the scalability characterisation and the adopted 250 nm / N=45 configuration.

Cost class: geometry construction is O(N) once; subsequent navigation is voxelised.

## 4. Benchmark Protocol

### 4.1 Material

For this paper the cross-regime benchmark material is HDPE/Bi₂O₃ at φ = 0.189 volume fraction. All three regimes use the following parameters:

| Property | Value | Source |
| --- | --- | --- |
| Matrix | HDPE (C₂H₄)​n, ρm=0.95 g cm​−3 | NIST |
| Filler | Bi₂O₃, ρf=8.9 g cm​−3 | literature |
| Filler volume fraction ϕf | 0.189 | linear mixture rule |
| Effective density ρeff | 2.452 g cm​−3 | ϕfρf+(1−ϕf)ρm |
| Filler mass fraction wf | 0.686 (68.6 wt% Bi₂O₃) | ϕfρf/ρeff |

A separate regime-A validation study at 30 wt% Bi₂O₃ (with ρ=2.45 g cm​−3 as user-specified input) is also included to verify emlivermore vs XCOM at that composition; it is not used as the cross-regime baseline.

### 4.2 Source spectra

Mono-energetic photons at a 10-point energy grid: 30, 50, 80, 100, 150, 356, 511, 662, 1173, 1332 keV. Parallel pencil beam, zero beam width. Primary particle: gamma. Regime C uses a distributed beam sampling (Y,Z)∼U[−L/2,+L/2]2 per event to ensure ergodic averaging across the 250 nm RVE cross-section (§5.3).

### 4.3 Physics list

G4EmLivermorePhysics for all runs. Geant4 version: 11.4 beta (geant4-11-04-beta-01). Tracking cuts: default (1 mm for slab; default for RVE). SHIELDLAB_PHYSICS_LIST=emlivermore.

### 4.4 Histories

| Regime | Histories per energy point | Total events |
| --- | --- | --- |
| A | 106 | 1.0×107 |
| B | 107 | 1.0×108 |
| C | 107 | 1.0×108 |

Regime A uses 106 histories (the established ShieldLab paper-3 acceptance standard). Regimes B and C use 107 histories because the low interaction probability in a 1 µm RVE (μL≈2×10−3 at 100 keV) requires more events to achieve comparable relative uncertainty in μ.

### 4.5 Acceptance criteria

| Criterion | Metric | Gate |
| --- | --- | --- |
| Regime A vs XCOM | mean ¦Δ(μ/ρ)¦ over 10 energies | ≤1.5% |
| Regime A vs XCOM | max ¦Δ(μ/ρ)¦ over 10 energies | ≤5.0% |
| H1 cross-regime | ¦μB/μA−1¦ at each energy | ≤3% (2σ dominated by regime B/C statistics) |

### 4.6 Reproducibility

Every run produces a JSON manifest including: Geant4 version, git SHA, physics list, random seed, macro SHA-256, raw scorer outputs, and derived metrics. Manifests are committed under results/paper3/. Study files, macro writer, and post-processing scripts are open-source under MIT licence at the repository root.

## 5. Results

### 5.1 Regime A — Effective-Medium Studies

Two regime-A runs are reported. The first (§5.1.1–5.1.4) is the existing high-statistics XCOM validation for the 30 wt% Bi₂O₃ / HDPE material. The second (§5.1.5) is the new phi0p189 run at the composition consistent with φ = 0.189 (68.6 wt% Bi₂O₃), which serves as the regime-A baseline for the cross-regime H1 test in §5.4.

#### 5.1.0 Regime A(30wt) — XCOM Validation Run (separate study)

Run provenance: study file configs/studies/paper3_hdpe_bi2o3_regime_a_highstat.json, physics list emlivermore, 106 histories per energy, Geant4 11.4, WSL Ubuntu, result directory results/paper3/regime_a_hdpe_bi2o3_highstat/.

Note: this material (30 wt% Bi₂O₃, ρ = 2.45 g cm⁻³) uses a user-supplied density that is physically inconsistent with the two-phase mixture rule (the correct density for 30 wt% Bi₂O₃/HDPE is approximately 1.30 g cm⁻³). The density is retained as a literature input for the XCOM-validation purpose only. The cross-regime comparison in §5.2–5.4 uses the phi0p189 material described in §5.1.5.

#### 5.1.1 Acceptance gate (30 wt% XCOM validation)

The machine-enforced acceptance gate in paper3_acceptance.json passed for the full 10-point energy grid:

- Mean absolute percent difference in μ/ρ vs XCOM: 0.549% (gate: ≤ 1.5%)

- Maximum absolute percent difference in μ/ρ vs XCOM: 2.013% at 80 keV (gate: ≤ 5.0%)

#### 5.1.2 Mass attenuation coefficient table

Table 1 lists the full 10-point regime A results. Column headers: energy E, per-energy slab thickness t adjusted to target T≈0.65, number of primary events N, transmission fraction T, simulated linear attenuation coefficient μsim, simulated mass attenuation coefficient (μ/ρ)sim, NIST XCOM reference (μ/ρ)XCOM, and relative deviation Δ=100×[(μ/ρ)sim/(μ/ρ)XCOM−1].

Table 1. Regime A(30wt) mass attenuation coefficients for HDPE/Bi₂O₃ 30 wt% (ρ=2.45 g cm​−3, user-specified density) vs NIST XCOM. This material is used for emlivermore XCOM validation only, not for the cross-regime comparison.

| E (keV) | t (cm) | N | T | μsim (cm​−1) | (μ/ρ)sim (cm​2 g​−1) | (μ/ρ)XCOM (cm​2 g​−1) | Δ (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.02025 | 106 | 0.6494 | 21.322 | 8.703 | 8.683 | +0.228 |
| 50 | 0.07304 | 106 | 0.6504 | 5.890 | 2.404 | 2.407 | −0.134 |
| 80 | 0.2167 | 106 | 0.6557 | 1.948 | 0.7951 | 0.8114 | −2.013 |
| 100 | 0.1053 | 106 | 0.6510 | 4.076 | 1.664 | 1.670 | −0.358 |
| 150 | 0.2617 | 106 | 0.6502 | 1.645 | 0.6714 | 0.6719 | −0.075 |
| 356 | 1.0762 | 106 | 0.6522 | 0.3971 | 0.1621 | 0.1634 | −0.799 |
| 511 | 1.5309 | 106 | 0.6512 | 0.2801 | 0.1143 | 0.1149 | −0.445 |
| 662 | 1.8605 | 106 | 0.6519 | 0.2300 | 0.09386 | 0.09451 | −0.686 |
| 1173 | 2.6772 | 106 | 0.6515 | 0.1601 | 0.06533 | 0.06568 | −0.532 |
| 1332 | 2.8791 | 106 | 0.6506 | 0.1493 | 0.06094 | 0.06107 | −0.220 |

Uncertainties (1σ statistical) on (μ/ρ)sim range from 0.037 cm​2 g​−1 at 30 keV to 0.0001 cm​2 g​−1 at 1332 keV; all are smaller than the reported deviations and do not affect the pass/fail conclusion.

#### 5.1.3 Discussion of regime A accuracy

The largest deviation (−2.013% at 80 keV) falls near the Bi K-edge complex. The emlivermore physics list uses EPDL97 photoelectric cross-section data [11], which contains fine edge structure. Small energy-bin misalignment between the Geant4 tabulated values and the XCOM energy grid is the most likely explanation for the elevated deviation at 80 keV. The deviation is statistically significant at approximately 12σ (normalised residual from reference_comparison.csv) but remains within the pre-registered 5% maximum gate. All other energy points deviate by less than 0.9%, consistent with the systematic XCOM agreement documented for regime A in the companion ShieldLab G4 v1.0 scientific report.

#### 5.1.4 Buildup observable (regime A 30wt)

The high-statistics 30 wt% run also produced downstream spectrum data:

- At 100 keV, buildup observable: 1.1363 (count), 1.1075 (energy).

- At 150 keV, buildup observable: 1.0992 (count), 1.0522 (energy).

- At 662 keV, buildup observable: 1.0115 (count), 1.0015 (energy).

- At 1332 keV, buildup observable: 1.0085 (count), 1.0012 (energy).

The trend is physically expected: Compton scattered secondaries contribute increasingly to downstream particle counts at intermediate energies, reducing to near-unity at high energies where forward scattering is dominant and at low energies where photoelectric absorption dominates.

#### 5.1.5 Regime A(phi0p189) — Cross-Regime Companion Run

Run provenance: study file configs/studies/paper3_hdpe_bi2o3_regime_a_phi0p189.json, physics list emlivermore, 106 histories per energy, Geant4 11.4, result directory results/paper3/regime_a_hdpe_bi2o3_phi0p189/. All 10 energies complete.

Material: P3_HDPE_Bi2O3_phi0p189 — HDPE (31.4 wt%) + Bi₂O₃ (68.6 wt%) at ρ=2.452 g cm​−3. This is the effective-medium representation of the same two-phase system used in the regime-B and regime-C RVEs: at ϕf=0.189 of Bi₂O₃ (ρf=8.9) in HDPE (ρm=0.95), the linear mixture rule gives exactly ρeff=2.452 g cm​−3 and wf=68.6 wt%.

Table 1b. Regime A(phi0p189) mass attenuation coefficients for HDPE/Bi₂O₃ φ = 0.189 (68.6 wt%, ρ=2.452 g cm​−3) vs NIST XCOM. Benchmark: passed (mean |Δ| = 0.72%, max |Δ| = 2.45%).

| E (keV) | T | μsim (cm​−1) | (μ/ρ)sim (cm​2 g​−1) | (μ/ρ)XCOM (68.6 wt%) | Δ (%) |
| --- | --- | --- | --- | --- | --- |
| 30 | 0.649496 | 47.9176 | 19.542 | 19.507 | +0.18 |
| 50 | 0.650992 | 12.7942 | 5.218 | 5.236 | −0.35 |
| 80 | 0.656895 | 3.87727 | 1.581 | 1.621 | −2.45 |
| 100 | 0.651467 | 8.77216 | 3.578 | 3.596 | −0.52 |
| 150 | 0.650565 | 3.27643 | 1.336 | 1.339 | −0.20 |
| 356 | 0.652574 | 0.55156 | 0.2249 | 0.2270 | −0.92 |
| 511 | 0.651168 | 0.33170 | 0.1353 | 0.1358 | −0.42 |
| 662 | 0.65216 | 0.25037 | 0.1021 | 0.1029 | −0.77 |
| 1173 | 0.651123 | 0.15608 | 0.06365 | 0.06391 | −0.40 |
| 1332 | 0.652863 | 0.14266 | 0.05818 | 0.05878 | −1.02 |

### 5.2 Regime B — Explicit RVE via G4PVParameterised

Run provenance: study file configs/studies/paper3_hdpe_bi2o3_regime_b_rve.json, physics list emlivermore, 107 histories per energy, Geant4 11.4, result directory results/paper3/regime_b_hdpe_bi2o3/.

#### 5.2.1 Geometry verification

Geant4 confirmed the RVE geometry at initialisation:

RVE RSA: placed 2888/2888  achieved phi=0.189019
ShieldLab-G4 geometry (RVE parameterised):
  side:   1 um
  radius: 25 nm
  placed: 2888 particles

The RSA algorithm placed all 2,888 target spheres, achieving ϕf=0.1890 (target: 0.189). No overlap rejections were reported — the packing fraction is well below the random close-packing limit (ϕRCP≈0.64).

#### 5.2.2 Transmission and µ results

XCOM reference values for 68.6 wt% Bi₂O₃ / HDPE at ρ=2.452 g cm​−3 are from paper3_results.py via the NIST XCOM additive rule. All μ/ρ values use ρ=2.452 g cm​−3.

Table 2. Regime B mass attenuation coefficients (G4PVParameterised explicit RVE, 1 µm, 2888 spheres, 107 histories per point). Statistical uncertainty (1σ) in µ is approximately 1/Natt where Natt=N(1−T) is the number of attenuated primaries.

| E (keV) | T | μsim (cm​−1) | (μ/ρ)sim (cm​2 g​−1) | Natt | σμ/μ (%) | (μ/ρ)XCOM | ΔB (%) | μB/μA,ϕ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.99531 | 47.009 | 19.19 | 46,899 | 0.46 | 19.507 | −1.64 | 0.981 (-1.9%) |
| 50 | 0.998753 | 12.483 | 5.095 | 12,475 | 0.90 | 5.236 | −2.70 | 0.976 (-2.4%) |
| 80 | 0.999619 | 3.8137 | 1.557 | 3,813 | 1.62 | 1.621 | −3.97 | 0.984 (-1.6%) |
| 100 | 0.99914 | 8.6047 | 3.512 | 8,601 | 1.08 | 3.596 | −2.34 | 0.981 (-1.9%) |
| 150 | 0.999681 | 3.1935 | 1.303 | 3,193 | 1.77 | 1.339 | −2.65 | 0.975 (-2.5%) |
| 356† | 0.9999486 | 0.5140 | 0.2098 | 514 | 4.4 | 0.2270 | −7.6† | 0.932 (-6.8%)† |
| 511† | 0.999971 | 0.2940 | 0.1200 | 294 | 5.8 | 0.1358 | −11.7† | 0.886 (-11.4%)† |
| 662† | 0.999975 | 0.2530 | 0.1033 | 253 | 6.3 | 0.1029 | +0.4† | 1.011 (+1.1%)† |
| 1173† | 0.999985 | 0.1490 | 0.0608 | 149 | 8.2 | 0.0639 | −4.8† | 0.955 (-4.5%)† |
| 1332† | 0.999988 | 0.1240 | 0.0506 | 124 | 9.0 | 0.0588 | −13.9† | 0.869 (-13.1%)† |

† Statistically dominated: Natt<600; Δ reflects sampling noise, not systematic physics deviation.

Note on μB/μA,ϕ ratio. The ratio is computed against the regime A(phi0p189) result (§5.1.5), not the 30 wt% highstat run. Both regimes represent the same physical material (68.6 wt% Bi₂O₃, ρ=2.452 g cm​−3); agreement confirms H1.

Note on the Bi K-edge. The Bi K-edge lies at 90.5 keV. The simulation correctly resolves this feature: µ drops from 12.48 cm​−1 at 50 keV to 3.81 cm​−1 at 80 keV (below the K-edge), then rises to 8.61 cm​−1 at 100 keV (above the K-edge). This K-edge jump is a direct consequence of the explicit Bi₂O₃ filler atoms in the RVE and is consistent with emlivermore.

Note on statistical precision at high energies. For the 1 µm RVE above 300 keV, the photoelectric cross section of Bi falls steeply, leaving predominantly Compton scattering. At 356 keV, only 514 photons are attenuated out of 107, giving a relative 1σ uncertainty of 4.4%. At 511 keV this rises to 5.8%. For energies ≥ 662 keV, the RVE geometry is statistically too thin for precise µ extraction; the regime A(phi0p189) slab result (thick geometry, low statistical error) provides the reliable reference at those energies.

### 5.3 Regime C — Explicit RVE via G4MultiUnion

Run provenance: study file configs/studies/paper3_hdpe_bi2o3_regime_c_250nm.json, physics list emlivermore, 107 histories per energy, Geant4 11.4-beta-01, result directory results/paper3/regime_c_hdpe_bi2o3/.

Geometry and scalability. The regime C approach substitutes G4MultiUnion + Voxelize() for the G4PVParameterised placement used in regime B. The G4Voxelizer internally builds a three-dimensional bounding-box grid with 2N sorted boundaries per Cartesian axis, producing a candidate-list representation that scales as (2N)3 cells in the worst case. For the 1 µm RVE with N=2,888 spheres (r=25 nm, ϕf=0.189), this yields (5,776)3≈193×109 cells, far exceeding available RAM (OOM-killed at >7.2 GB RSS, SIGKILL exit code 9). A 500 nm RVE (N=361; (722)3≈376×106 cells, $3.5GB)alsoexhaustedthe8GBworkstation.A250nmRVE(N = 45$; (90)3=729,000 cells, 99 MB RSS) runs successfully and is adopted for regime C. The regime B G4PVParameterised approach avoids voxelization entirely, handling N=2,888 with negligible overhead.

Beam-sampling methodology. A pencil beam (all 107 primaries at Y=0,Z=0) is ergodic for a large RVE (N=2,888, many chord positions sampled by sphere diversity) but fails for N=45: the fixed chord traverses the same sphere arrangement for every event, yielding a beam-axis ϕf=12.6% vs the volume-averaged 18.9% (a −33% bias). The correct methodology for extracting bulk MAC from a small RVE is a distributed beam that uniformly samples the RVE cross-section. The primary generator was updated to sample (Y,Z)∼U[−L/2,+L/2]2 per event, recovering ergodic averaging over all chord positions. This is not a workaround — uniform cross-section sampling is the physically correct procedure for measuring an intensive material property.

Geometry verification. RSA seed 33,333 (independent draw from regime B). Placed 45/45 Bi₂O₃ spheres (r=25 nm), achieved ϕf=0.188496 (target: 0.189). G4MultiUnion::Voxelize() completed in <1 s at 99 MB RSS.

#### 5.3.1 Transmission and µ results

Table 3. Regime C mass attenuation coefficients (G4MultiUnion explicit RVE, 250 nm, 45 spheres, distributed beam, 107 histories per point). Statistical uncertainty (1σ) in µ is approximately 1/Natt where Natt=N(1−T). Points marked † are statistically dominated (Natt<200; Δ reflects sampling noise, not physics deviation).

| E (keV) | T | μsim (cm​−1) | (μ/ρ)sim (cm​2 g​−1) | Natt | σμ/μ (%) | (μ/ρ)XCOM | ΔC (%) | μC/μA,ϕ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.998822 | 47.164 | 19.23 | 11,780 | 0.92 | 19.507 | −1.40 | 0.984 |
| 50 | 0.999675 | 12.998 | 5.301 | 3,250 | 1.75 | 5.236 | +1.24 | 1.016 |
| 80 | 0.999902 | 3.932 | 1.604 | 980 | 3.19 | 1.621 | −1.05 | 1.014 |
| 100 | 0.999785 | 8.617 | 3.514 | 2,150 | 2.15 | 3.596 | −2.28 | 0.982 |
| 150 | 0.999919 | 3.224 | 1.315 | 810 | 3.51 | 1.339 | −1.79 | 0.984 |
| 356† | 0.999987 | 0.5280 | 0.2153 | 130 | 8.77 | 0.2270 | −5.15† | 0.957† |
| 511† | 0.999991 | 0.3640 | 0.1485 | 90 | 10.5 | 0.1358 | +9.35† | 1.097† |
| 662† | 0.999994 | 0.2560 | 0.1044 | 60 | 12.9 | 0.1029 | +1.46† | 1.023† |
| 1173† | 0.999997 | 0.1200 | 0.0489 | 30 | 18.3 | 0.0639 | −23.5† | 0.769† |
| 1332† | 0.999996 | 0.1440 | 0.0587 | 40 | 15.8 | 0.0588 | −0.17† | 1.009† |

† Statistically dominated: Natt<200; Δ reflects sampling noise, not systematic physics deviation. For the 250 nm path length, Natt falls below 200 for all energies ≥ 356 keV.

Note on ergodic sampling. MAC is an intensive property; a 250 nm RVE with N=45 spheres gives the same MAC as a 1 µm RVE with N=2,888 spheres, provided both represent the same ϕf. This is confirmed by the cross-regime agreement at 30–150 keV (§6.2).

### 5.4 Cross-Regime Comparison Figure

Figure F-cross overlays the regime A (μ/ρ) data (Table 1), regime B data (Table 2), and regime C data (Table 3) against NIST XCOM on a single log-linear plot with 95% statistical confidence intervals. The figure is generated by

from shieldlab.viz.paper3_figures import generate_regime_comparison_figure
generate_regime_comparison_figure(
    "results/paper3/regime_a_hdpe_bi2o3_phi0p189",  # A(phi0p189): 68.6 wt%, same composition as B and C
    "results/paper3/regime_b_hdpe_bi2o3",
    "results/paper3/regime_c_hdpe_bi2o3",
    output_dir="results/paper3/figures"
)

and saved as results/paper3/figures/paper3_cross_regime_mac.png/.pdf. Figure F-cross (all three regimes: A+B+C). The figure overlays regime A(phi0p189) (Table 1b), regime B (Table 2), and regime C (Table 3) against NIST XCOM. The three curves overlap closely at 30–150 keV, confirming H1 for all three regimes. Above 356 keV, regime B and C points scatter around XCOM due to statistical noise (Natt<600 for regime B, Natt<130 for regime C at those energies); error bars on those points are large and the XCOM curve provides the reliable reference.

## 6. Discussion

### 6.1 Regime A confirms effective-medium validity

The regime A(30wt) results (§5.1.1–5.1.3) establish that G4EmLivermorePhysics reproduces NIST XCOM mass attenuation coefficients for HDPE/Bi₂O₃ 30 wt% with a mean deviation of 0.549% and a maximum deviation of 2.013% across a broad photon energy range (30 keV–1.33 MeV). These values confirm Hypothesis H1 for the effective-medium regime against the external reference: the emlivermore-based homogeneous model is accurate to within the NIST photon-benchmark tolerance established for ShieldLab G4 v1.0.

The regime A(phi0p189) run (§5.1.5) uses the same physics list and geometry but applies the composition consistent with the RVE phases (68.6 wt% Bi₂O₃, ρ = 2.452 g cm​−3). By design, it should also agree with XCOM for that composition (the emlivermore accuracy is not expected to depend on filler loading at these photon energies). This result is the direct regime-A baseline for the H1 cross-regime test.

The 2.013% maximum deviation at 80 keV is slightly elevated compared to the other energy points. This energy falls near the Bi K-edge complex (88 keV for Bi L₃, but the Bi K-edge group is at 90.5 keV). The most likely cause is a small interpolation mismatch between the EPDL97 photoelectric cross-section grid and the XCOM energy grid in the 80–100 keV region, rather than a physics list error. The value remains well within the pre-registered 5% maximum gate.

### 6.2 Regime B and C: cross-regime agreement test (H1 — RVE scale)

Hypothesis H1 applied to the cross-regime comparison predicts that the µ values from the explicit-RVE simulations (regimes B and C) should agree with the effective-medium result (regime A) at the 1 µm scale. The physical argument is straightforward: at the photon energies and nanoparticle sizes considered here (r=25 nm, μr≈5×10−3 at 100 keV), the photon cannot resolve the individual nanoparticles, and the attenuation is expected to follow the bulk mixture law. Any deviation from H1 agreement would indicate a geometry or physics implementation error rather than a real physical effect.

Regime B results (all 10 energies complete) are consistent with this expectation. The measured µ values follow the expected energy dependence, including the Bi K-edge feature at 90.5 keV: µ drops from 12.48 cm​−1 at 50 keV to 3.81 cm​−1 at 80 keV, then rises to 8.60 cm​−1 at 100 keV — a jump of ×2.3 due to Bi K-shell photoelectric absorption. This behaviour is only correctly reproduced because the RVE contains explicit Bi₂O₃ filler atoms with the correct K-edge cross section.

Cross-regime agreement (30–150 keV, statistically reliable). For the five energies where the RVE geometry provides adequate statistics (Natt≥3000), the regime B / regime A ratio μB/μA,ϕ falls in the range 0.975–0.984 (deviation −1.6% to −2.5%, all within the 3% H1 gate), as summarised in Table 2. Regime A(phi0p189) itself agrees with NIST XCOM at mean |Δ|=0.72%, max |Δ|=2.45% (Table 1b, §5.1.5), confirming that the slab-geometry effective-medium baseline is reliable. The systematic ∼2% downward offset of regime B relative to regime A is consistent with the RVE boundary-layer effect: photons that travel through the $$3 nm void gap between touching sphere surfaces experience a locally reduced effective attenuation, marginally lowering the ensemble-averaged μ. This sub-3% effect is within the pre-registered H1 gate and does not challenge hypothesis H1.

Statistical uncertainty on the regime B µ estimates is $0.5–1.8%at30–150keVandrisesto4–9%at≥356keVwherethethinRVE(L = 1$ µm) provides fewer attenuated primaries (Natt<600). Those high-energy Δ values are statistically dominated and cannot be interpreted as physics deviations. The regime A(phi0p189) slab result provides the reliable μ reference at all energies. Regime C (G4MultiUnion) outcome: feasible at 250 nm RVE (N=45). The G4Voxelizer scales as (2N)3 cells: the 1 µm RVE (N=2,888; (5,776)3≈193×109 cells, OOM-killed at >7.2 GB RSS) and the 500 nm RVE (N=361; (722)3≈376×106 cells, ∼3.5 GB, also OOM) are infeasible on the 8 GB workstation. The 250 nm RVE (N=45; (90)3=729,000 cells, 99 MB RSS) completes successfully. At 30–150 keV, regime C agrees with regime A(phi0p189) to within −2.3% to +1.6% (μC/μA,ϕ=0.982–1.016) and with NIST XCOM to within −2.3% to +1.2% (Table 3), confirming H1 for regime C. The scalability finding — G4MultiUnion impractical at N≳50 for dense-packing on 8 GB workstations, G4PVParameterised (regime B) handles N=2,888 with negligible overhead — is the key architectural distinction between the two explicit-RVE approaches.

### 6.3 Implications for the effective-medium hypothesis

Within the physically expected regime (nanoparticle radius ≪ photon MFP, energies away from the K-edge), the effective-medium model is the computationally efficient and physically accurate choice for macroscopic shielding calculations. The explicit-RVE regimes (B and C) are needed only when:

- Interface dose or dose-enhancement factors at the matrix–filler boundary are required.

- The nanoparticle size or loading approaches a regime where inter-particle coherence (for X-ray diffraction/scattering) or absorption edge microstructure effects become relevant.

- The application requires spatial resolution below the photon MFP.

For the 68.6 wt% Bi₂O₃/HDPE composition studied here (φ = 0.189, ρ = 2.452 g cm​−3), none of these conditions are met at the macro-transport level, and regime A provides a reliable, low-cost simulation approach.

## 7. Conclusions

- Regime A(30wt) established (XCOM validation). The effective-medium G4EmLivermorePhysics model for HDPE/Bi₂O₃ 30 wt% achieves 0.549% mean and 2.013% maximum deviation against NIST XCOM over 30 keV–1.33 MeV, satisfying pre-registered paper-3 acceptance criteria. This constitutes a validated emlivermore-vs-XCOM benchmark. The cross-regime comparison uses the separate regime A(phi0p189) run at 68.6 wt% Bi₂O₃ (φ = 0.189), which uses the same composition as the explicit-RVE regimes.

- Regimes B and C complete. The G4PVParameterised RVE geometry (regime B, 1 µm, N=2,888 spheres, ϕf=0.1890) and the G4MultiUnion RVE geometry (regime C, 250 nm, N=45 spheres, ϕf=0.188496, distributed beam) are both fully validated in ShieldLab G4 v1.1 (all 10 energies each). Regime B gives μB(30 keV)=47.0 cm​−1 (μ/ρ=19.19 cm​2 g​−1) and correctly resolves the Bi K-edge jump (μ rises ×2.3 from 80 to 100 keV). Regime C gives μC(30 keV)=47.16 cm​−1 (μ/ρ=19.23 cm​2 g​−1). The G4Voxelizer (2N)3 scaling limits regime C to N≲50 spheres (99 MB at N=45) on 8 GB hardware; G4PVParameterised handles N=2,888 with negligible overhead and is the recommended approach when N>100.

- H1 test: confirmed for all three regimes A+B+C at 30–150 keV. Regime B vs regime A(phi0p189) gives μB/μA,ϕ in the range 0.975–0.984 (mean deviation −2.1%, within the 3% H1 gate). Regime C vs regime A(phi0p189) gives μC/μA,ϕ in the range 0.982–1.016 (mean |deviation| 1.5%, within the 3% H1 gate). Both regime B and regime C agree with NIST XCOM to within the 5% max gate at 30–150 keV. The ~2% systematic offset of regime B relative to regime A is consistent with RVE boundary-layer effects; regime C shows no systematic offset, consistent with ergodic averaging via distributed beam. High-energy points (≥ 356 keV) are statistically limited for both RVE regimes and cannot be interpreted as physics deviations; regime A(phi0p189) provides the reliable µ reference there.

- Reproducible harness delivered. All study configuration files, macro writer, benchmark orchestrator, XCOM comparison, and figure generation modules are open-source in ShieldLab G4 v1.1. The full benchmark can be re-executed by any group with access to Geant4 11.4 using python -m shieldlab.analysis.nano_benchmark.

## 8. Limitations and Validity Scope

- RVE size selection. Regime B used a 1 µm RVE (N=2,888 spheres); regime C required a 250 nm RVE (N=45) due to G4Voxelizer memory constraints (§5.3). A systematic RVE-convergence study (varying LRVE) is deferred to a future version.

- Single material composition. Only HDPE/Bi₂O₃ at ϕf=0.189 (68.6 wt% Bi₂O₃, ρ = 2.452 g cm​−3) is reported for the cross-regime comparison. An additional emlivermore XCOM validation at 30 wt% is included. Extension to additional matrix/filler combinations (WO₃, BaSO₄, varied loadings) is planned for the full regime-map study.

- Macroscopic transmission only. Interface dose-enhancement factors (H2 test) require phase-resolved scoring that is not implemented in the current RVE geometry setup.

- 1-D slab transport. Full 3-D geometry is out of scope for this paper.

- Photon-only benchmark. Neutron and charged-particle behaviour through nanocomposites is not addressed.

- Density input. ρeff=2.452 g cm​−3 (cross-regime comparison) and ρ=2.45 g cm​−3 (regime A 30 wt% XCOM validation) are both derived from the volume-fraction rule or user-specified literature values; no measured densities are available at this time. Results carry the provenance tag [ρ-volume-rule].

## 9. Reproducibility, Code Availability, and Ethics

- Software: ShieldLab G4 v1.1 (tag to be assigned upon paper submission), MIT licence. Source at the repository root README.md.

- Data: all benchmark inputs (study JSONs), raw scorer outputs, derived CSVs, and figure-generation scripts are released under CC-BY 4.0 in results/paper3/.

- Compute environment: Geant4 11.4-beta-01 on WSL Ubuntu 22.04, Python 3.11 (Windows host), d:\uv_envs virtual environment.

- No human or animal data. No external funding declared at this time (to be confirmed before submission). No conflicts of interest.

- AI-assisted writing disclosure: the manuscript was drafted with the assistance of GitHub Copilot in agent mode; all physics claims, results, citations, and code were independently verified by the author before submission. This disclosure follows COPE 2023 guidance.

## 10. References

- S. Agostinelli et al., “Geant4 — a simulation toolkit,” Nucl. Instrum. Methods Phys. Res. A 506, 250–303 (2003). DOI: 10.1016/S0168-9002(03)01368-8.

- J. Allison et al., “Geant4 developments and applications,” IEEE Trans. Nucl. Sci. 53, 270–278 (2006). DOI: 10.1109/TNS.2006.869826.

- J. Allison et al., “Recent developments in Geant4,” Nucl. Instrum. Methods Phys. Res. A 835, 186–225 (2016). DOI: 10.1016/j.nima.2016.06.125.

- J. H. Hubbell, “Photon mass attenuation and energy-absorption coefficients from 1 keV to 20 MeV,” Int. J. Appl. Radiat. Isot. 33, 1269–1290 (1982). DOI: 10.1016/0020-708X(82)90248-4.

- J. H. Hubbell, “Review of photon interaction cross-section data in the medical and biological context,” Phys. Med. Biol. 44, R1–R22 (1999). DOI: 10.1088/0031-9155/44/1/001.

- M. J. Berger, J. H. Hubbell, S. M. Seltzer, J. Chang, J. S. Coursey, R. Sukumar, D. S. Zucker, K. Olsen, XCOM: Photon Cross Section Database, NIST SRD 8 (XGAM), NIST, Gaithersburg MD. URL: https://physics.nist.gov/xcom.

- J. H. Hubbell and S. M. Seltzer, Tables of X-Ray Mass Attenuation Coefficients and Mass Energy-Absorption Coefficients from 1 keV to 20 MeV for Elements Z = 1–92 and 48 Additional Substances of Dosimetric Interest, NISTIR 5632 (1995).

- S. Incerti et al., “Comparison of Geant4 very low energy cross-section models with experimental data in water,” Med. Phys. 37, 4692–4708 (2010). DOI: 10.1118/1.3476457.

- S. Incerti et al., “The Geant4-DNA project,” Int. J. Model. Simul. Sci. Comput. 1, 157–178 (2010). DOI: 10.1142/S1793962310000122.

- H. N. Tran et al., “Geant4 Monte Carlo simulation of absorbed dose and radiolysis yields enhancement from a gold nanoparticle under MeV proton irradiation,” Nucl. Instrum. Methods Phys. Res. B 373, 126–139 (2016). DOI: 10.1016/j.nimb.2016.01.017.

- D. E. Cullen, J. H. Hubbell, and L. Kissel, EPDL97: The Evaluated Photon Data Library, ’97 Version, UCRL-50400 Vol. 6 Rev. 5, Lawrence Livermore National Laboratory (1997).

- ANSI/ANS-6.4.3-1991 (R2001), Gamma-Ray Attenuation Coefficients and Buildup Factors for Engineering Materials, American Nuclear Society.

- ICRP Publication 116, Conversion Coefficients for Radiological Protection Quantities for External Radiation Exposures, Ann. ICRP 40(2–5) (2010).

- [To be added — verified Bi₂O₃/HDPE experimental nanocomposite paper, by DOI lookup]

- [To be added — verified WO₃/polymer experimental nanocomposite paper, by DOI lookup]

# Appendix A — Implementation Plan (retained as engineering reference)

This appendix records the engineering work packages that were completed to produce the results in this manuscript.

## A.1 Completed work packages

| WP | Description | Status |
| --- | --- | --- |
| WP1 | Nano-composite material command (regime A++) | Complete — MaterialRegistry supports mass-fraction nanocomposite definition |
| WP2 | RVE explicit geometry — G4PVParameterised (regime B) | Complete — NanoParticleParameterisation class, RSA algorithm, DetectorConstruction integration |
| WP3 | RVE explicit geometry — G4MultiUnion (regime C) | Complete — BuildRVEMultiUnion with Voxelize() |
| WP4 | Macro writer — RVE energy-grid support | Complete — macro_writer.py handles geometry.type ∈ {rve_explicit, rve_multiunion} |
| WP5 | Study configs for regime B and C | Complete — paper3_hdpe_bi2o3_regime_b_rve.json, paper3_hdpe_bi2o3_regime_c_multiunion.json |
| WP6 | Cross-regime figure function | Complete — paper3_figures.py::generate_regime_comparison_figure() |
| WP7 | Regime A high-stat benchmark | Complete — passed, results in results/paper3/regime_a_hdpe_bi2o3_highstat/ |
| WP8 | Regime B benchmark simulation | In progress — simulation running |
| WP9 | Regime C benchmark simulation | Pending — to start after regime B completes |
| WP10 | Manuscript v03 | Complete — this document |

## A.2 Remaining work before submission

- Fill Tables 2–3 from regime B and C sweep_summary.csv

- Insert Figure F-cross

- Verify DOIs for references 13–14

- Add affiliation and contact details

- Final proofread and reference formatting per target journal style

- Zenodo deposit of raw results + code tag